Part I

QUALITY ASSURANCE – Brick Tests

- All tests shall be in accordance with ASTM C-67 latest edition

Submittals

- Test reports shall include:

  - Compressive strength

  - 24-hour cold water absorption.

  - 5-hour boil absorption

  - Saturation Coefficient

  - Initial Rate of Absorption (IRA)

  - Weather classification

- Certificate of conformance shall state that brick meets or exceeds applicable ASTM specifications indicated herein.

Sample Panels

- Sample panel size shall be 4'x4' showing the proposed color range, texture, bond, mortar, workmanship, cleaning, and water repellents where applicable.

Part II

Facing Bricks

- All brick shown on contract documents shall be color, texture as manufactured by General Shale, PO Box 3547, 3015 Bristol Highway, Johnson City, TN 37602-3547.

- ASTM C-216 latest edition, Grade SW, Type FBS or ASTM C-652 latest edition, Grade SW, Type HBS, Class H40V.

- Dimensions 31/2"x 21/4"x 75/8" (W x H x L)

Structural Bricks

- All brick shown on contract documents shall be color, texture as manufactured by General Shale, PO Box 3547, 3015 Bristol Highway, Johnson City, TN 37602-3547.

- ASTM C-652 latest edition, Grade SW, Type HBS, Class H40V.

- Dimensions 55/8"x 23/4"x 115/8" (W x H x L)

Thin Bricks

- All brick shown on contract documents shall be color, texture as manufactured by General Shale, PO Box 3547, 3015 Bristol Highway, Johnson City, TN 37602-3547.

- ASTM C-1088 latest edition, Exterior Grade, Type TBX (except for chips) .

- Dimensions 1/2"x 2 1/4"x  7 5/8" (W x H x L)

Shapes

- Where special shapes are shown on architectural drawings, manufacturer shall provide shop drawings for architect’s approval prior to manufacturing shapes.

Mortar

Mortar shall be type consisting by proportion:

Part Portland cement (ASTM C-150 Type I or II)

Part hydrated lime (ASTM C-207)

Parts sand (ASTM C-144)

Grout

Grout shall conform to ASTM C-476 for fine grout mix. Slump shall be 10"

- Part Portland cement (ASTM C-150, Type I or II)

- 1/4 to 3 parts sand (ASTM C-404)

Part III

EXECUTION

- Bond - Bond shall be running bond unless otherwise shown on contract documents.

- Jointing - Mortar joints shall be concave and struck with a smooth steel tool.

- Construction - All construction strictly adheres to (ACI 530)

- Cleaning - Cleaning shall conform to Technical Bulletin 4: Section 4200, Brick Cleaning Recommendations and to BIA Technical Note #20-R. Contact manufacturer for recommendations.

- Water Repellent & Coatings - Where water repellents are specified consult Technical Bulletin 1: Section 1700, Water Repellent Coatings.